## Slide 1: Double-Double laminates for improved impact and post-impact resistance
Dongwon Lee
Avin Vijay

## Slide 2: Quasi-isotropic laminates
What is quasi-isotropic laminates?
Quasi-isotropic
  Quasi means “almost” and Isotropic means that material that behaves the same in all direction.
Why do we need Quasi-isotropic?
Design
  Only using 0, 45, -45, 90 orientation
  Lacking rational basis– extension of isotropic mechanics
  Weight penalty

## Slide 3: Double-Double (DD) Laminates
Double-double laminates have
  Most general orientation is
  Can have other permutations or symmetry
  No need to enforce mid-plane symmetry
  Homogeneous
  Balanced and minimal [D]
  Efficient manufacturing
  Easy to rework
What are double-double laminates and its benefits?
Notes: [+"θ" _1,- "θ" _1,+ "θ" _1,- "θ" _1,+ "θ" _2,- "θ" _2,+ "θ" _2,- "θ" _2]

## Slide 4: Impact and Compression After Impact
Low velocity impact/ BVID- typical to occur in service like tool drops.
The CAI test simulates real-world damage scenarios that could occur in service.
The goal is to evaluate how much compressive load a composite laminate can carry after sustaining such damage
Two stages
  Impact stage
  Compression stage

## Slide 5: Mechanics Problem
u
A flat, rectangle panel
  6 in x 4 in
Simply supported on lateral edges
Clamped at x=0,a
Load applied from x=a
Material Properties
Toray T800/3900S
Each lamina will have thickness of 0.0075 in
Density 1.44 x inch-lbf-s

## Slide 6: and Orientations
Total of 16 plies
5 different cases
  Case 1 :
  Case 2 :
  Case 3 :
  Case 4 :
  Case 5 :

## Slide 7: Buckling vs. Transition Loads
, the critical load, is the minimum load at which a structure switches stable load paths due to buckling
can be obtained through linear eigenvalue buckling analysis
For symmetric laminates, lowest eigenvalue reliably predicts the critical buckling loads
Load vs end-shortening
Solid line
  Ideal (perfect) structure
  Theoretical equilibrium path is symmetric
Dashed line
  Real (imperfect) structure
  Realistic response with small initial imperfections or load eccentricity

## Slide 8: Transition Loads
With initial imperfection, the structure smoothly shifts into a buckling mode
Transition load often governs usable capacity more than
Lager imperfection will give lower transition load
Bending loads & Unsymmetry → Coupling
Bending loads arise from external moments, eccentricity, or thickness/geometry variations
Unsymmetric laminate → membrane-bending coupling (B≠0)
  In-plane forces N induce curvatures κ
  Moments M induce mid-plane strains
Notes: Why “transition load” matters “Real parts aren’t perfectly straight or flat. With an initial imperfection, the structure doesn’t suddenly snap at 𝑃_𝑐𝑟; it gradually moves into a buckled mode. The load at which that shift becomes dominant is the transition load. In design, this value often governs the usable capacity more than the theoretical 𝑃_𝑐𝑟. And importantly, a bigger imperfection means a lower transition load.”
Where bending loads come from “Even if we intend pure in-plane loading, bending appears due to applied moments, eccentric load paths, or thickness/geometry variations—all common in manufacturing and assembly.”
Unsymmetry ⇒ coupling “If the laminate is unsymmetric, we get membrane–bending coupling. Physically: in-plane forces 𝐍 induce curvature 𝜿; applied moments 𝐌 induce mid-plane strains 𝜺^0. Mathematically, that’s the B-matrix effect: with 𝐁≠0for unsymmetric stacks.”

## Slide 9: Imperfection seeding
Sinusoidal model
Generalized Imperfect seeding
  Obtain buckling mode shape from Eigen value analysis
  Scaling one or more of these mode shapes as initial geometric imperfections in a subsequent nonlinear static analysis.
  Identify the from the plot
What if some layups are not symmetric?
If it is non-symmetric, we cannot use eigenvalue.
  It overestimates the critical load
  Miss the actual buckling mode
  B matrix in stiffness matrix is not zero
Notes: Some layups are unsymmetric, so a simple linear eigenvalue buckling analysis can be misleading. With membrane–bending coupling (∗∗𝐵≠0∗∗), the linear eigenvalue model tends to over-predict the critical load and can miss the actual buckling path. In practice, we introduce an initial imperfection and run a nonlinear static analysis to capture the real transition into buckling.
The workflow is:
Run a linear buckling analysis to obtain mode shapes.
Seed the geometry with a scaled combination of those modes as the initial imperfection.
Perform a nonlinear static (e.g., Riks/arc-length) analysis and read off the transition load 𝑃_"transition" from the load–deflection curve.
This approach reflects how imperfect structures actually behave: they ease into a buckled configuration, and the transition load—not the ideal 𝑃_𝑐𝑟—often governs usable capacity.”
The lowest plate buckling modes for common boundary conditions are sinusoidal, so it matches the shape with the least energy and what the eigenproblem predicts.

## Slide 10: Optimization workflow
Stage 0 : Create sample input file
  B.C.s
  Material Properties
Stage 1 : Python Pre-Process
  Imperfection seeding
  Orientation
Stage 2 : .inp Generation & Abaqus Run
Stage 3 : .dat & .odb
  or
  ω
Stage 4 : Post-Processing & QC
  Check if is correct by looking at the xy plot
Stage 5 : Output & Data Management
  Generate .csv file to save data
Notes: Given ply orientation, using python script, the abaqus will run the buckling/imperfection analysis.
From either .dat or .odb file, 𝑷_𝒄𝒓 can be obtained.
After 200 runs, we will see which orientation will have highest value.

## Slide 11: Type 1: Imperfection perfect
=
Type 1: Imperfection perfect
Characteristics
  Initial stiffness is nearly linear
  Post-transition stiffness is also approximately linear
  Knee point is clear and stable
Decision: Transition load = intersection of the initial and post-transition fitted lines.

## Slide 12: Type 2: Imperfection imperfect - 1
Type 2: Imperfection imperfect - 1
=
=
Characteristics
  Initial stiffness is nearly linear
  Post-transition stiffness curves
  Knee point is somewhat unclear
  Need to look at u3 displacement plot
Decision: Transition load = (intersection of the initial and post-transition fitted lines from force plot + intersection of initial and post-transition fitted lines from u3 plot) / 2
U3 displacement plot

## Slide 13: Type 3: Imperfection imperfect - 2
Type 3: Imperfection imperfect - 2
=
=
Characteristics
  Initial stiffness is nearly linear
  Post-transition stiffness curves heavily
  Knee point is somewhat unclear
  Need to look at u3 displacement plot
Decision: Transition load = intersection of initial and post-transition fitted lines from u3 plot
U3 displacement plot

## Slide 14: Three different types and selection rule
Type | Curve behavior | U3 usage | Final transition load
Type 1 | Clear bilinear curve | Not necessary | Use bilinear intersection
Type 2 | Somewhat bilinear, but second region curves | Necessary | 
Type 3 | Bilinear fitting is unreliable | Necessary | u3-based transition load only
Type | Curve behavior | U3 usage | Final transition load
Type 1 | Clear bilinear curve | Not necessary | Use bilinear intersection
Type 2 | Somewhat bilinear, but second region curves | Necessary | 
Type 3 | Bilinear fitting is unreliable | Necessary | u3-based transition load only
Check force-displacement curve
Clear Bilinear?
Unclear knee point with somewhat curve second region
Second region curves heavily?
Type 1
Yes
No
Type 2
Yes
No
Type 3
Yes

## Slide 15: Result Overview: 5 Cases, 2 Surface Patterns
Pattern I: Case 1 & 5
Pattern II: Case 2, 3 & 4
Case 1
Case 5
Similar twin-ridge /
Center basin pattern
Case 2
Case 3
Case 4
4-corner peak structure with a low center region
Key contrast
+28.93% vs Quasi
Case 3 best / quasi = 15916.5 / 12344.8
Design implication
±45º-type angles dominates
High-performing regions appear away from ==0º

## Slide 16: Pattern I: Case 1 & 5
Case 1
Case 5
Shared visual pattern
Center basin + Side ridges
Both surfaces favor nonzero ±θ combinations
Highest case 1
15,386.6
=40.53º, =-50.32º
Highest case 5
15,484.1
Quasi | Benchmark | 12,344.8
Case 1 | Best | 15,386.6
Case 5 | Best | 15,484.1
Case 5 | vs Quasi | +25.41%
Case 5 | vs [0/0] | +186.42%
Case 5 | vs Case 1 | +0.63%
Case 5 slightly improves the peak while preserving the same response shape
=-43.13º, =-44.92º

## Slide 17: Pattern II: Case 2, 3 & 4
Case 2
Case 3
Quasi | Benchmark | 12,344.8
Case 2 | Best | 15,880.6
Case 3 | Best | 15,916.5
Case 4 | Best | 15,908.5
Case 3 | vs Quasi | +28.93%
Case 3 | vs [0/0] | +194.42%
Case 3 | vs Case 2 | +0.22%
Case 3 | vs Case 4 | +0.05%
Case 4
Cases 2, 3, and 4 highest peak is located near =44.13º and =-49.42º
Shared visual pattern
4-corner peak with a low center region
All surfaces favor nonzero ±θ combinations
range
15.88k – 15.91k
Small variation among cases

## Slide 18: Ranking: Optimized Layups vs. Benchmarks
Chart: Best 𝑷cr/𝑷tr by Case vs. Benchmarks
Case 1 | 15386.6
Case 2 | 15880.6
Case 3 | 15916.5
Case 4 | 15908.5
Case 5 | 15484.1
Quasi | 12344.8
[0/0] | 5406
[90/90] | 4628
Improvement vs quasi
+28.93%
15916.5 compare with 12344.8
Highest
Case 3: 15,916.5
=44.13º, =-49.42º
Improvement vs Case 5
+2.79%
15916.5 compare with 15484.1
All optimized layups cluster around 15.8k, while [0/0] and [90/90] are much lower. Therefore, the main result is not only which case wins, but that the optimized ±θ angle family consistently outperforms the basic baselines.

## Slide 19: Best Result : Case 3
Best
15916.5 lbs
44.13 | -49.42 | 15,916.5
51.32 | 45.92 | 15,652.3
-43.13 | -44.92 | 15485.3
-46.72 | 63.91 | 15072.8
44.13 | -49.42 | 15,916.5
51.32 | 45.92 | 15,652.3
-43.13 | -44.92 | 15485.3
-46.72 | 63.91 | 15072.8
Top candidate list
=44.13º, =-49.42º
vs [0/0]
+194.42%
2.94x higher than baseline
vs Quasi
+28.93%
1.28x higher than quasi-isotropic
The high- region occurs around ±45°-type asymmetric combinations, not near the [0/0] or [90/90] baselines.

## Slide 20: Cost function evaluation
QI:
= 12344.8 lbs
ω = 1113.5 Hz
To maximize bending and membrane stiffnesses, a weighted cost function is used
  A static non-linear analysis predicts the realistic transition loads
  An eigen value analysis predicts the fundamental frequency in lieu of flexural rigidity
Each term is normalized to its reference , then weighted (70% buckling, 30% flexural rigidity) to match project priorities.
Higher scores indicate more superior designs.
QI evaluated using the same criteria
Notes: The objective function was defined as a weighted normalized sum of the buckling/transition load and natural frequency. A weighting factor of 0.7 was assigned to the buckling or transition load because structural stability was the primary design objective, while a weighting factor of 0.3 was assigned to the natural frequency as a secondary dynamic performance criterion.

## Slide 21: Result Overview: 5 Cases, 2 Surface Patterns
Pattern I: Case 1 & 5
Pattern II: Case 2, 3 & 4
Case 1
Case 5
Similar twin-ridge /
Center basin pattern
Case 2
Case 3
Case 4
4-corner peak structure with a low center region
Key contrast
+31.31% vs Quasi
Case 2 best / quasi = 2.998788 / 2.283682
Design implication
±45º-type angles dominates
High-performing regions appear away from ==0º

## Slide 22: Pattern I: Case 1 & 5
Case 1
Case 5
Shared visual pattern
Center basin + Side ridges
Both surfaces favor nonzero ±θ combinations
Highest case 1
2.894787
=43.23º, =-49.42º
Highest case 5
2.902941
Quasi | Benchmark | 2.283682
Case 1 | Best | 2.894787
Case 5 | Best | 2.902941
Case 5 | vs Quasi | +27.12%
Case 5 | vs [0/0] | +190.29%
Case 5 | vs Case 1 | +0.28%
Case 5 slightly improves the peak while preserving the same response shape
=-43.13º, =-44.92º

## Slide 23: Pattern II: Case 2, 3 & 4
Case 2
Case 3
Quasi | Benchmark | 2.283682
Case 2 | Best | 2.998788
Case 3 | Best | 2.993270
Case 4 | Best | 2.993247
Case 2 | vs Quasi | +31.31%
Case 2 | vs [0/0] | +199.88%
Case 2 | vs Case 3 | +0.18%
Case 2 | vs Case 4 | +0.19%
Case 4
Cases 2, 3, and 4 highest peak is located near =44.13º and =-49.42º
Shared visual pattern
4-corner peak with a low center region
All surfaces favor nonzero ±θ combinations
range
2.9932 – 2.9987
Small variation among cases

## Slide 24: Ranking: Optimized Layups vs. Benchmarks
Chart: Best f by Case vs. Benchmarks
Case 1 | 2.8948
Case 2 | 2.9988
Case 3 | 2.9933
Case 4 | 2.9932
Case 5 | 2.9029
Quasi | 2.2837
[0/0] | 1
[90/90] | 1.5962
Improvement vs quasi
+31.31%
15916.5 compare with 12344.8
Highest
Case 2: 2.998788
=44.13º, =-49.42º
Improvement vs Case 5
+3.3%
2.998788 compare with 2.902941
All optimized layups cluster around 2.9, while [0/0] and [90/90] are much lower. Therefore, the main result is not only which case wins, but that the optimized ±θ angle family consistently outperforms the basic baselines.

## Slide 25: Best Result : Case 2
Best
2.988788
44.13 | -49.42 | 2.998788
51.32 | 45.92 | 2.956361
-46.72 | 63.91 | 2.927417
-57.52 | -49.42 | 2.925126
44.13 | -49.42 | 2.998788
51.32 | 45.92 | 2.956361
-46.72 | 63.91 | 2.927417
-57.52 | -49.42 | 2.925126
Top candidate list
=44.13º, =-49.42º
vs [0/0]
+199.88%
2.99x higher than baseline
vs Quasi
+31.31%
1.31x higher than quasi-isotropic
The high- region occurs around ±45°-type asymmetric combinations, not near the [0/0] or [90/90] baselines.

## Slide 26: Result
The plot for case 1 and 5 being different was due to symmetry of layup.
Both case 1 and 5 have same theta values to be highest buckling load. However, case 5 had slightly higher critical buckling load value.
Between case 2, 3, and 4, case 3 has highest transition load value.
Overall, Case 3, , has highest transition load while Case 2, , has highest cost function value.

## Slide 27
Thank you!!
Questions??