## Slide 1: Double-Double laminates for improved impact and post-impact resistance
Dongwon Lee
Avin Vijay

## Slide 2: Quasi-isotropic laminates
What is quasi-isotropic laminates?
Quasi-isotropic
  Quasi means “almost” and Isotropic means that material that behaves the same in all direction.
Why do we need Quasi-isotropic?
Design
  Only using 0, 45, -45, 90 orientation
  Lacking rational basis– extension of isotropic mechanics
  Weight penalty

## Slide 3: Double-Double (DD) Laminates
What are double-double laminates and its benefits?
Double-double laminates have
  Most general orientation is
  Can have other permutations or symmetry
  No need to enforce mid-plane symmetry
  Homogeneous
  Balanced and minimal [D]
  Efficient manufacturing
  Easy to rework
Notes: [+"θ" _1,- "θ" _1,+ "θ" _1,- "θ" _1,+ "θ" _2,- "θ" _2,+ "θ" _2,- "θ" _2]

## Slide 4: Impact and Compression After Impact
Low velocity impact/ BVID- typical to occur in service like tool drops.
The CAI test simulates real-world damage scenarios that could occur in service.
The goal is to evaluate how much compressive load a composite laminate can carry after sustaining such damage
Two stages
  Impact stage
  Compression stage

## Slide 5: Mechanics Problem
A flat, rectangle panel
  6 in x 4 in
Simply supported on lateral edges
Clamped at x=0,a
Load applied from x=a
Material Properties
Toray T800/3900S
Each lamina will have thickness of 0.0075 in
u

## Slide 6: and Orientations
Total of 16 plies
3 different cases
  Case 1 :
  Case 2 :
  Case 3 :

## Slide 7: Buckling vs. Transition Loads
, the critical load, is the minimum load at which a structure switches stable load paths due to buckling
can be obtained through linear eigenvalue buckling analysis
For symmetric laminates, lowest eigenvalue reliably predicts the critical buckling loads
Load vs end-shortening
Solid line
  Ideal (perfect) structure
  Theoretical equilibrium path is symmetric
Dashed line
  Real (imperfect) structure
  Realistic response with small initial imperfections or load eccentricity

## Slide 8: Transition Loads
With initial imperfection, the structure smoothly shifts into a buckling mode
Transition load often governs usable capacity more than
Lager imperfection will give lower transition load
Bending loads & Unsymmetry → Coupling
Bending loads arise from external moments, eccentricity, or thickness/geometry variations
Unsymmetric laminate → membrane-bending coupling (B≠0)
  In-plane forces N induce curvatures κ
  Moments M induce mid-plane strains
Notes: Why “transition load” matters “Real parts aren’t perfectly straight or flat. With an initial imperfection, the structure doesn’t suddenly snap at 𝑃_𝑐𝑟; it gradually moves into a buckled mode. The load at which that shift becomes dominant is the transition load. In design, this value often governs the usable capacity more than the theoretical 𝑃_𝑐𝑟. And importantly, a bigger imperfection means a lower transition load.”
Where bending loads come from “Even if we intend pure in-plane loading, bending appears due to applied moments, eccentric load paths, or thickness/geometry variations—all common in manufacturing and assembly.”
Unsymmetry ⇒ coupling “If the laminate is unsymmetric, we get membrane–bending coupling. Physically: in-plane forces 𝐍 induce curvature 𝜿; applied moments 𝐌 induce mid-plane strains 𝜺^0. Mathematically, that’s the B-matrix effect: with 𝐁≠0for unsymmetric stacks.”

## Slide 9: Imperfection seeding
What if some layups are not symmetric?
If it is non-symmetric, we cannot use eigenvalue.
  It overestimates the critical load
  Miss the actual buckling mode
  B matrix in stiffness matrix is not zero
Generalized Imperfect seeding
  Obtain buckling mode shape from Eigen value analysis
  Scaling one or more of these mode shapes as initial geometric imperfections in a subsequent nonlinear static analysis.
  Identify the from the plot
Sinusoidal model
Notes: Some layups are unsymmetric, so a simple linear eigenvalue buckling analysis can be misleading. With membrane–bending coupling (∗∗𝐵≠0∗∗), the linear eigenvalue model tends to over-predict the critical load and can miss the actual buckling path. In practice, we introduce an initial imperfection and run a nonlinear static analysis to capture the real transition into buckling.
The workflow is:
Run a linear buckling analysis to obtain mode shapes.
Seed the geometry with a scaled combination of those modes as the initial imperfection.
Perform a nonlinear static (e.g., Riks/arc-length) analysis and read off the transition load 𝑃_"transition" from the load–deflection curve.
This approach reflects how imperfect structures actually behave: they ease into a buckled configuration, and the transition load—not the ideal 𝑃_𝑐𝑟—often governs usable capacity.”
The lowest plate buckling modes for common boundary conditions are sinusoidal, so it matches the shape with the least energy and what the eigenproblem predicts.

## Slide 10: Optimization workflow
Stage 0 : Create sample input file
  B.C.s
  Material Properties
Stage 1 : Python Pre-Process
  Imperfection seeding
  Orientation
Stage 2 : .inp Generation & Abaqus Run
Stage 3 : .dat & .odb
  ω
Stage 4 : Post-Processing & QC
  Check if is correct by looking at the xy plot
Stage 5 : Output & Data Management
  Generate .csv file to save data
Notes: Given ply orientation, using python script, the abaqus will run the buckling/imperfection analysis.
From either .dat or .odb file, 𝑷_𝒄𝒓 can be obtained.
After 200 runs, we will see which orientation will have highest value.

## Slide 11: Type 1: Imperfection perfect
We have perfect bilinear curve
Easy to tell plot and where transition load is located
=

## Slide 12: Type 2: Imperfection imperfect-1
We have somewhat bilinear curve
The 2nd part of the curve tends to “curve”
=

## Slide 13: Type 2: Imperfection imperfect-1
We will be looking at u3, the outer plane displacement, curve
We will use transition loads we get from “bilinear” and u3 to fine the “true transition load”
=

## Slide 14: Type 3: Imperfection imperfect-2
We have “bilinear curve” where we cannot use due to 2nd half of the curve has to much curve/slope
=

## Slide 15: Type 3: Imperfection imperfect-2
We will be looking at u3, the outer plane displacement, curve
We will only use transition loads we get from u3 and say this is our transition load
=

## Slide 16: Case 1:
Theta1 () | Theta2 () |  | % difference
Quasi-Isotropic : |  | 12334.13 lbs | standard
52.01 | 43.87 | 15246.84 lbs | 23.6%
-42.06 | -55.63 | 13469.28 lbs | 9%
-55.63 | 40.25 | 14515.84 lbs | 17.7%
46.58 | -42.06 | 15416.19 lbs | 25%
 |  |  | % difference
 |  | 12334.13 lbs | standard
52.01 | 43.87 | 15246.84 lbs | 23.6%
-42.06 | -55.63 | 13469.28 lbs | 9%
-55.63 | 40.25 | 14515.84 lbs | 17.7%
46.58 | -42.06 | 15416.19 lbs | 25%
Type 1 | Type 2 | Type 3
58 | 124 | 18

## Slide 17: Case 2:
Theta1 () | Theta2 () |  | % difference
Quasi-Isotropic : |  | 12334.13 lbs | standard
52.01 | 43.87 | 15353.86 lbs | 24.5%
-42.06 | -55.63 | 15025.73 lbs | 21.8%
-39.35 | 45.68 | 14788.71 lbs | 19.9%
47.49 | -42.06 | 15444.97 lbs | 25.2%
 |  |  | % difference
 |  | 12334.13 lbs | standard
52.01 | 43.87 | 15353.86 lbs | 24.5%
-42.06 | -55.63 | 15025.73 lbs | 21.8%
-39.35 | 45.68 | 14788.71 lbs | 19.9%
47.49 | -42.06 | 15444.97 lbs | 25.2%
Type 1 | Type 2 | Type 3
61 | 114 | 25

## Slide 18: Case 3:
Theta1 () | Theta2 () |  | % difference
Quasi-Isotropic : |  | 12334.13 lbs | standard
52.01 | 43.87 | 15266.21 lbs | 23.8%
-42.06 | -55.63 | 14921.66 lbs | 21%
-39.35 | -45.68 | 14615.84 lbs | 18.5%
46.58 | -42.06 | 15428.14 lbs | 25.1%
 |  |  | % difference
 |  | 12334.13 lbs | standard
52.01 | 43.87 | 15266.21 lbs | 23.8%
-42.06 | -55.63 | 14921.66 lbs | 21%
-39.35 | -45.68 | 14615.84 lbs | 18.5%
46.58 | -42.06 | 15428.14 lbs | 25.1%
Type 1 | Type 2 | Type 3
82 | 98 | 20

## Slide 19: Conclusions
Double-Double class of laminates as an alternative for design
DD laminates are more homogeneous and easy to manufacture
3 families of DD considered- with and without mid-plane symmetry
All 3 families of DD shows higher buckling loads than QI
Case 2:has the highest transition load in general than any other cases– 25.2% higher than QI family.

## Slide 20: Cost function evaluation
To maximize bending and membrane stiffnesses, a weighted cost function is used
  A static non-linear analysis predicts the realistic transition loads
  An eigen value analysis predicts the fundamental frequency in lieu of flexural rigidity
Each term is normalized to its reference , then weighted (70% buckling, 30% flexural rigidity) to match project priorities.
Higher scores indicate more superior designs.
QI evaluated using the same criteria
QI:
= 13595.78 lbs
ω = 6.5888 Hz

## Slide 21
Thank you!!
Questions??